Аннотация. Представлены результаты испытаний на сульфидно-оксидную коррозию при температурах 750-900ОС жаропрочных литейных никелевых сплавов для рабочих лопаток авиационных турбин с ионно-плазменными покрытиями. Показаны преимущества многослойных покрытий, полученных  с использованием сплавов на никелевой и алюминиевой основе, по сравнению с серийным однослойным покрытием из сплава на кобальтовой основе. Изучена микроструктура, состав покрытий после испытаний и определены некоторые характеристики прочности композиций сплав-покрытие.

Ключевые слова: суперсплавы, коррозионностойкие покрытия,  лопатки турбин

Abstract. The hot corrosion test of aviation turbine blades nickel superalloys with ion-plasma coatings at temperatures 750-900ОС were investigation. Advantages of the multilayer coats from nickel and aluminum alloys in comparison with a commercial overlay coating from cobalt alloy are shown. The microstructure, composition of coats after test is studied and some mechanical properties coated superalloy are spotted.

Keywords: superalloy, corrosion resistant coating, turbine blade